SECTION 07223

LOW SLOPE ROOFING COVER BOARD FOR MECHANICALLY ATTACHED SYSTEMS ONLY

** NOTE TO SPECIFIER **  Hunter Panels, manufacturers of rigid polyisocyanurate insulation for commercial and residential buildings including new construction and retrofit projects.  A universally accepted substrate for all major types of roof coverings Hunter panels offers the highest R-value per inch, superior compressive strength, and the best pricing of any insulating material on the planet.

This section is based on the products of Hunter Panels, which is located at:

15 Franklin Street

Portland, Maine 04101

Phone: (207) 761-5678 or (888) 746-1114

Fax: (877) 775-1769

E-mail: info@hpanels.com

Internet: www.hunterpanels.com

[click Here] for additional information.

Hunter Panels is the developer and producer of high performance flat and sloped polyisocyanurate insulation panels for flat roofing applications and is viable in green and sustainable building designs. This specification is for flat and tapered H-Shield a rigid roof insulation panel composed of a closed cell polyisocyanurate foam core bonded on each side to fiber reinforced facers.

This specification includes Hunter Panel’s new line of cover board products for new construction and reroofing applications and includes H-Shield HD - High-Density Cover Board and H-Shield HD Composite CG composed of 1/2 inch H-Shield HD Bonded to Premium Performance Polyiso insulation.

GENERAL

SECTION INCLUDES

** NOTE TO SPECIFIER **  Delete items below not required for project.

High Density Cover Board.

RELATED SECTIONS

** NOTE TO SPECIFIER **  Delete any sections below not relevant to this project; add others as required.

Section 07200 - Building Insulation.

Section 05300 - Steel Deck.

Section 06114 - Wood Blocking.

Section 06150 - Wood Decking.

Section 07222 - Polyisocyanurate Roof Insulation.

Section 07260 - Vapor Retarders.

Section 07530 - Electrometric Membrane Roofing.

Section 07540 - Thermoplastic Membrane Roofing.

REFERENCES

** NOTE TO SPECIFIER **  Delete references from the list below that are not actually required by the text of the edited section.

ASTM C 209 - Methods of Testing Insulating Board, Structural and Decorative.

ASTM C 518 - Standard Test Method for Steady-State Thermal Transmission Properties by Means of the Heat Flow Meter Apparatus

ASTM C 1289 - Standard Specification for Faced Rigid Cellular Thermal Insulation Board.

ASTM D 1621 – Test Methods for Compressive Properties of Rigid Cellular Plastics.

ASTM D 2126 - Test Method for Response of Rigid Cellular Plastics to Thermal and Humid Aging.

ASTM E 84 - Surface Burning Characteristics of Building Materials.

ASTM E 96 - Test Method for Water Vapor Transmission of Materials.

ASTM E 108 - Standard Tests Method for Fire Tests of Roof Coverings.

ASTM E 119 - Standard Test Methods For Fire Tests Of Building Construction and Materials.

FM Approval Guide - FM 4450 Approval Standard - Class I Insulated Steel Roof Decks.

FM Approval Guide - FM 4470 Approval Standard - Class I Roof Covering.

UL 263 - Fire Tests of Building Construction and Materials.

UL 790 - Tests for Fire Resistance of Roof Covering Materials.

UL 1256 - Fire Test of Roof Deck Constructions.

SUBMITTALS

Submit under provisions of Section 01300.

Product Data:  Manufacturer's data sheets on each product to be used, including:

Preparation instructions and recommendations.

Storage and handling requirements and recommendations.

Installation methods.

Shop Drawings: Roof plan layout of boards and fastening patterns.

** NOTE TO SPECIFIER **  Delete the following paragraphs if LEED is not applicable.

      - LEED Submittals:  Provide documentation of how the requirements of Credit will be met: List of proposed materials with recycled content.  Indicate post-consumer recycled content and pre-consumer recycled content for each product having recycled content.

      - Manufacturer-Specific Environmental Product Declaration which conforms to ISO 14025

Verification Samples:  For each finish product specified, two samples, representing actual product.

Submit 6 by 6 inch (152 mm by 152 mm) samples of each board type required.

Submit samples of each fastener type required.

    - Manufacturer's Certificate:  Certify panels will conform to specified performance requirements.

QUALITY ASSURANCE

    - Manufacturer Qualifications: Manufacturer shall be a company that regularly manufactures and assembles specified insulation in house with no outside fabrication operations.

    - Manufacturer shall have multiple manufacturing facilities to ensure consistency of product supply.

DELIVERY, STORAGE, AND HANDLING

Good construction practice dictates that all insulations should be protected from moisture and direct sunlight during job-site storage. Pallets of Hunter Panels H-Shield HD-MA products are protected by a 2-step packaging process using shrink wrap and a UV resistant polyethylene bag. This moisture resistant package is designed for protection from the elements during flatbed shipment from our facilities to the job-site.

Store products in accordance with the manufacturer recommendations.

Store product on a solid flat foundation and elevate a minimum of 2 inches above the finished surface.

Slit the bundle packaging vertically down the center of the two short sides and cover with a waterproof tarpaulin.

Protect insulation from open flame and keep dry at all times.

PROJECT CONDITIONS

Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results.  Do not install products under environmental conditions outside manufacturer's absolute limits.

Do not apply cover board insulation or roofing materials when substrate is damp or wet or when proper adhesive temperature cannot be maintained.

COORDINATION

Coordinate work with installation of insulation, roof covering and associated roof penetrations and counterflashings installed by other sections as work of this section proceeds.

PRODUCTS

MANUFACTURERS

Basis of Design:  Hunter Panels, 15 Franklin Street, Portland, Maine 04101.

Phone: (207) 761-5678 or (888) 746-1114.  Fax: (877) 775-1769.  E-mail: info@hpanels.com. Web: www.hunterpanels.com.

** NOTE TO SPECIFIER **  Delete one of the following two paragraphs; coordinate with requirements of Division 1 section on product options and substitutions.

Substitutions:  Not permitted.

Requests for substitutions will be considered in accordance with provisions of Section 01600.

MATERIALS

Roof Board Insulation: Provide products that comply with the following:

** NOTE TO SPECIFIER ** Delete all of the following standards that are not required; coordinate with product specifications.

ASTM standards specified.

Factory Mutual (FM) approvals specified.

Underwriters Laboratories Inc. (UL) classifications specified.

California Code of Regulations, Title 24, Insulation Quality Standard License #TI-1420

** NOTE TO SPECIFIER ** Select one or more of the cover board types as required for the project from the following paragraphs. Delete the paragraphs that are not required. Suitable for new roofing applications and retrofit applications when existing materials are left in place. Compatible with Single-Ply Roofing Systems (fully adhered and mechanically attached), and Modified Bitumen Roofing Systems. Suitable for use with approved fastener and plates, also cold applied and low-rise adhesives. Not approved for application directly to steel deck.

High Density Cover Board: Flat H-Shield HD-MA; high density polyiso insulation panel with Glass Fiber-Reinforced Facers (GRF) specifically designed for use as a cover board in mechanically attached systems. Manufactured per ASTM C 1289, Type II, Class 1.

Manufactured using 3rd Generation Zero ODP, EPA Compliant Blowing Agent; Contains zero CFCs, HCFCs, or HFCs; Virtually no Global Warming Potential (GWP)

Properties:

Compressive Strength: ASTM D 1621, Grade 3 (25psi minimum)

Dimensional Stability: ASTM D 2126, < 2 percent linear change in 7 days.

Water Absorption: ASTM C 209, < 3 percent volume.

Service Temperature: 260 degrees F or less.

Recycled Content: > 9 percent.

Weight: 0.3431 lbs/sq ft

Panel Size: 48 inches by 96 inches (1220 mm by 2440 mm).

Thickness: 0.50 inch (13 mm),

R Value: R Value 2.5 as tested in accordance with ASTM C 518.

Codes and Compliances:

** NOTE TO SPECIFIER ** Consult with applicable Code for specific assembles.

UL Classified 790.

ASTM E 108.

FM Approved.

ACCESSORIES

Approved Fasteners: Appropriate for purpose intended and approved by FM Approvals and system manufacturer; length required for thickness of insulation material and penetration of deck substrate, with distribution plates if required.

Base Ply: As recommended by membrane manufacturer.

EXECUTION

Do not begin installation until substrates have been properly prepared.

Examine roof deck for suitability to receive cover board. Verify that substrate is dry, clean, and free of foreign material that will damage installation.

Verify that roof drains, scuppers, roof curbs, nailers, equipment supports, vents, and other roof accessories are secured properly and installed in conformance with drawings and submittals.

Verify that deck is structurally sound to support installers, materials, and equipment without damaging or deforming work.

If substrate preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation before proceeding.

PREPARATION

Clean surfaces thoroughly prior to installation.

Prepare surfaces using the methods recommended by the manufacturer for achieving the best result for the substrate under the project conditions.

** NOTE TO SPECIFIER **  The incorporation of a vapor barrier or retarder within the roofing assembly is highly recommended when the project is located in Zones 1, 2 or 3 of the United States. H-Shield is not intended to substitute for a vapor barrier. Vapor barrier or retarder when used shall have a perm rating of 0.5 or less as determined by ASTM E 96.

Apply vapor barrier and or retarder, as specified by the Architect or required by the local building code, to decking prior to installation of insulation.

INSTALLATION

Install specified cover board in accordance with manufacturer's latest printed instructions and as required by governing codes and Owner's insurance carrier.

Do not leave installed cover board exposed to weather. Cover and waterproof immediately after installation.

Seal exposed joints at the end of each day. Remove seal when work resumes.

Remove installed cover board that has become wet or damaged and replace with new solid and dry material.

** NOTE TO SPECIFIER ** Select one of the following three installation system paragraphs for the roof system required and delete the ones not required. Edit each system as required by the governing codes and Owners insurance requirements. Coordinate with the requirements of the roof system manufacturer. Note that H-Shield HD and H-Shield HD Composite CG is intended for use with single ply ballasted and mechanically attached systems only.

Mechanically Attached Single-Ply Systems:

Each cover board panel must be secured to the roof deck with Factory Mutual approved fasteners and plates (appropriate to the deck type).

Butt edges and stagger joints of adjacent panels.

** NOTE TO SPECIFIER ** Include the following paragraph for subsequent insulation systems if required. Delete if not required.

Roof Insulation: Install subsequent layers of roof insulation as specified in Section 07222.

Install the roof covering according to the roof manufacturer's specifications.

** NOTE TO SPECIFIER ** Note the following paragraph applies only to H-Shield HD Composite CG. Delete if not applicable.

** NOTE TO SPECIFIER ** Note the following paragraph can apply to H-Shield HD or H-Shield HD Composite CG. H-Shield HD Composite CG provides a singular and sustainable solution in retrofit applications when existing insulation is left in place. To facilitate compliance with ASHRAE 90.1 Standards for energy efficiency, H-Shield HD Composite CG can be installed in a single layer on top of intact and dry insulation after the Single-Ply membrane is removed. The new Single-Ply membrane can then be installed over an insulation assembly that complies with the latest energy code requirements.

Re-roofing Single-Ply systems:

Remove existing single ply membrane and clean surface of debris or irregularities.

Verify that the existing insulation is dry and sound.

Install coverboard insulation in a single layer on top of intact and dry insulation.

Butt edges and stagger the joints in accordance with good roofing practice and fasten as per manufacturer’s specifications.

Install the new Single-Ply membrane according to the roof manufacturer's specifications.

For multiple layered installations, install the base layer of panels loose-laid, and stagger the joints of subsequent layers in accordance with good roofing practice.

CLEANING

Remove trash and construction debris from insulation before application of roofing membrane.

PROTECTION

Protect installed products until completion of project.

Protect installed board traffic by use of protective covering materials during and after installation.

Cover the top and edges of unfinished roof panel work to protect it from the weather and to prevent accumulation of water under the panels. Only apply enough cover board per day that can be covered by the finished roof system.

Do not leave panels exposed to moisture. Wet panels shall be removed or allowed to completely dry prior to application of vapor barrier and/or roof covering.

Repair or replace damaged products before Substantial Completion.

END OF SECTION